Revised October 18, 2018

A FEW THERMODYNAMIC CONSIDERATIONS FOR MATERIALS

by Paul Paslay, P.E. #44278 (inactive)

I.  INTRODUCTION

A requirement from physical science is that any theory describing material behavior must conform to the general results from Thermodynamics.  The purpose of this report is to tie the results given in the file “Classical Thermodynamics” (October 17, 2015, THERMO.DOC) to continuum mechanics and to determine any conditions that must be imposed on constitutive equations and corresponding internal energies in order for them to conform to Classical Thermodynamics.

In the case of a continuum mechanics formulation for a particular the system studied is a fixed mass particle.  The stresses and strains are considered to be uniform.  The first essential part for this study concerns the First Law of Thermodynamics for fixed mass systems which may be expressed as,

ρ⋅q = E + W

where definitions and a compatible set of units for this equation are (note that mass is any  mass unit),

	= mass density, massin3

q	= time rate of heat flow into the differential mass, in−lbfmass-sec

ρ⋅q	= time rate of heat flow into the differential volume, in−lbfin3−sec

= ρ⋅T⋅s for a reversible process

E	= differential volume time rate of change of internal (strain) energy, in−lbfin3−sec

W	= time rate of work being done by the system on differential volume, in−lbfin3−sec

In addition, define,

T	= absolute temperature, oR

ρ⋅s	= qT = time rate of reversible change of entropy, in−lbfin3−sec - oR

ρ⋅sTOT	= qTOTT = time rate of change of total entropy, in−lbfin3−sec - oR

To provide some background, briefly consider the elementary case of combined, linear heat transfer and conduction.  Let cV in−lbfmass-oR be the specific heat and K in−lbfin-sec−oR the heat flux rate per unit volume and define I oRin2  as,

I = n=13T,nn       (n=1,2,3 = x, y, z)

where I is the Laplacian of T.  The reversible heat flow rate, qREV, is,

ρ⋅qREV = ρ⋅cV⋅T+K⋅I

Since there is no work done by this system,

W = 0

and the First Law of Thermodynamics is,

qREV = E

The two equations for qREV show that E is a function of T and I.  Then,

E = ∂ E∂T⋅T+∂ E∂I⋅I = ρ⋅cV⋅T+K⋅I = ρ⋅cV⋅T+K⋅n=1n=3T,nn

Consequently,

E = ρ⋅cV⋅T+ K⋅I

and,

s = qREVT = cV⋅TT+K⋅n=1n=3T,nnT

When a specific constitutive equation is considered, it is often possible to express W explicitly.  Substituting W into the first law and solving for the reversible part of s yields an equation whose validity must be determined.  The condition that the entropy, s, be a perfect differential (i.e. s is a property dependent only on the state of the material and thus path independent) leads to a condition that must be satisfied by E.  When this condition is satisfied then the Inequality of Clausius is valid and it becomes a way of expressing the Second Law of Thermodynamics as,

ds ≥ 0

where the equality is only for a reversible cycle.

Several common, elementary, constitutive equations are reviewed in the section below.  In each case, the expressions for E, s and sTOT are determined.  In each case, the derivation is given in Cartesian spatial coordinates.  These reviews show the kind of restrictions thermodynamics imposes on constitutive equations undergoing changes of state.

The results below use the common indicial notation for the subscripts i, j, k, and m.  A comma preceding subscripts implies partial differentiation with respect to the subscript variable.  Additionally, a repeated subscript occurring in a single term implies summation over x, y and z for that term.

Let ij be the Kronecker delta defined as,

δij = 1 when i=j = 0 when i≠j

then a few examples using indicial notation are,

δij⋅δij = 3

σij⋅δij = σkk = σxx+σyy+σzz

σi,i = ∂ σi∂xi = ∂ σx∂x+∂ σy∂y+∂ σz∂z

σVM2 = J2 = 32⋅σij−13⋅σkk⋅δij⋅σij−13⋅σkk⋅δij = 32⋅σij⋅σij−13⋅σkk2 = σxx2+σyy2+σzz2−σxx⋅σyy−σyy⋅σzz−σzz⋅σxx+3⋅σxy2+σyz2+σzx2

II.  SELECTED, ILLUSTRATIVE, CONSTITUTIVE EQUATIONS

A.  LINEAR THERMOELASTICITY

This constitutive equation relates the strains, eij, stresses, sij, and absolute temperature, T, as,

σij = λ⋅ekk − 3⋅α⋅T⋅δij + 2⋅G⋅eij − α⋅T⋅δij = λ⋅ekk⋅δij+2⋅G⋅eij− 3⋅λ+2⋅G⋅α⋅T⋅δij

where in terms of the material constants Young’s modulus, E, and Poisson’s ratio, ,

λ = ν⋅E1 + ν⋅1 − 2⋅ν

G = E2⋅1 + ν

3⋅λ+2⋅G = E1−2⋅ν

E = G⋅3⋅λ+2⋅Gλ

ν = λ2⋅G+λ

and the inverse of the constitutive equation is,

eij = 12⋅G⋅σij + −μ2⋅1+μ⋅G⋅σkk+α⋅T⋅δij = 12⋅G⋅σij + −λ2⋅G⋅3⋅λ+2⋅G⋅σkk+α⋅T⋅δij

 = thermal coefficient of linear expansion, a constant = ρ⋅∂∂T1ρ , 1oR

 = mass density, a function of eij and T,  massin3

The parameters λ, G and α are constants so that, up to this point the internal energy, E, and density,  are functions of eij and T.

The thermodynamic system under consideration is a particle whose volume is constant.  The rate of work per unit volume done by this particle on its exterior is,

W = −σij⋅eij

Now assume the internal energy per unit volume is a function of eij and T so that,

E = ∂ E∂eij⋅eij + ∂ E∂T⋅T

and the Thermodynamic First Law gives,

q = E + W = ∂ E∂eij − σij⋅eij + ∂ E∂T⋅T

The reversible entropy production rate, s, is,

s = qT = 1T⋅∂ E∂eij − σij⋅eij + 1T⋅∂ E∂T⋅T

In order that s be a state function, the following condition must be satisfied,

∂∂T1T⋅∂ E∂eij − σij= ∂∂eij1T⋅∂ E∂T

The order of differentiation may be reversed so that,

∂ E∂eij = σij − T⋅∂ σij∂T

When the thermoelasticity constitutive equation given above is substituted into this condition, the result is,

∂ E∂eij = λ⋅ekk⋅δij + 2⋅G⋅eij

Integration of ∂ E∂eij gives,

E = 12⋅λ⋅ekk2 + G⋅eij⋅eij + HT

then,

q = 3⋅λ + 2⋅G⋅α⋅T⋅ekk + ∂ HT∂T⋅T

s = 3⋅λ + 2⋅G⋅α⋅ekk + ∂ HT∂T⋅TT

In order to relate H(T) to a physically familiar quantity, note that T is an independent thermodynamic property and when the strain rates are zero the value of q is,

q|eij = 0 = ∂ HT∂T⋅T ≡ cVT

where cV is the specific heat at constant volume and assumed to be constant.  Then. H(T) may be written as,

HT = cV⋅T − TO

where cV⋅TO is a constant of integration.  Consequently, E may be written as,

E = 12⋅λ⋅ekk2 + G⋅eij⋅eij+ cV⋅T − TO

and,

q = 3⋅λ + 2⋅G⋅α⋅T⋅ekk + cV⋅T

s = 3⋅λ + 2⋅G⋅α⋅ekk + cV⋅TT

and, since there is no energy dissipation in the material,

sTOT = s = 3⋅λ + 2⋅G⋅α⋅ekk + cV⋅TT

The temperature, T, is the absolute temperature in the above derivation.  When the constitutive equation is used in problem solving, it is common to replace (T-TO) with a temperature that is not a true thermodynamic temperature (e.g. degrees Celsius).

B.  LINEAR, VISCOUS, COMPRESSIBLE NEWTONIAN FLUID

The constitutive equation for this fluid may be written in terms of the stress, ij, the strain, eij, the deformation rate, eij, and the absolute temperature, T, in the form,

σij = λ⋅ekk⋅δij + 2⋅μ⋅eij + C⋅ekk − 3⋅α⋅T⋅δij

where,

λ and μ	= volumetric and shear viscosities, constant material properties

C		= elastic compressibility, constant material property

- = thermal coefficient of linear expansion, a constant

This case of a fluid introduces new considerations to the determination of the internal energy and the entropy functions.  The presence of a viscosity implies that there is a dissipation of energy within the material element owing to flow.  When the system is dissipative the entropy function cannot be derived using the constitutive equation in the same way as given in the case of the thermoelastic material.  By assuming that E is a function of eij, eij and T and proceeding in the same way as the thermoelastic material derivation shows there is no entropy function that is a state variable.  When dissipation is present it is converted to heat and this must be reflected in the contributions to the First Law of Thermodynamics.  From a physical point of view, the total work done by the stresses can be divided into two parts.  The first part of the work is that which is required to make the entropy a state variable.  The second part of the work is the excess of the total work over the first part.  The second part is converted to external heat and is not included in the first law equation for the material particle.  This may, in this case, be accomplished by splitting the stress into two parts, Dij and Sij.  The stress , Dij, is determined from the part of the constitutive equation causing dissipation while the stress,  Sij, is determined from the part of the constitutive equation contributing to the recoverable elastic strain energy as follows,

σij = σDij + σSijσDij = λ⋅ekk⋅δij + 2⋅μ⋅eij σSij = C⋅ekk − 3⋅α⋅T⋅δij

The rate of work per unit volume being done by the system is −σSij⋅eij.  Assume the internal energy is a function of ekk and T so that the First Law of Thermodynamics gives,

q = ∂ E∂ekk⋅ekk + ∂ E∂T⋅T − σSij⋅eij = ∂ E∂ekk⋅δij − σSij⋅eij + ∂ E∂T⋅T

and the entropy production rate, s, is

s = 1T⋅∂ E∂ekk⋅δij − σSij⋅eij + ∂ E∂T⋅TT

In order for the entropy to be a state property,

−1T2⋅∂ E∂ekk⋅δij − σSij + 1T⋅∂2 E∂T∂ekk⋅δij − ∂ σSij∂T = 1T⋅∂2 E∂eij∂T = 1T⋅∂2 E∂ekk∂T⋅δij

The order of differentiation for the second derivatives is interchangeable so this equation becomes,

T⋅∂ σSij∂T − σSij = −∂ E∂ekk⋅δij

When the constitutive equation for Sij is substituted into the above equation, the result is,

∂ E∂ekk = C⋅ekk

The last equation is integrated to give,

E = 12⋅C⋅ekk2 + JT

where J(T) is an arbitrary function of T.  When E is substituted into the expressions for heat flow rate and entropy production rate given above, the expressions become,

q = 3⋅α⋅T⋅C⋅ekk + d JTdT⋅T

s = 3⋅α⋅C⋅ekk + d JTdT⋅TT

When ekk = 0, the heat flow rate is usually written as cV⋅T with cV being the specific heat.  In this case,

d JTdT = cV

Since cV is assumed to be a constant, integration yields,

JT = cV⋅T − TO

where cv⋅TO is a constant of integration.  To summarize,

q = 3⋅α⋅T⋅C⋅ekk + cV⋅T

s = 3⋅α⋅C⋅ekk + cV⋅TT

E = 12⋅C⋅ekk2+ cV⋅T − TO

The value of q in these equations is the total heat flow rate for the system and some is generated internally while the remainder is supplied externally to the material element.  The internal heat flow rate, qD, is,

qD = σDij⋅eij= λ⋅ekk⋅δij + 2⋅μ⋅eij⋅eij

Now let the externally supplied heat flow rate be q so that,

q = q + qD

and,

q = 3⋅α⋅T⋅C⋅ekk + cV⋅T + λ⋅ekk2 + 2⋅μ⋅eij⋅eij

and then,

sTOT = qT = 3⋅α⋅C⋅ekk + cV⋅TT + λT⋅ekk2 + 2⋅μT⋅eij⋅eij

The rate of entropy change for the dissipation, sDISS, equals sTOT−s or,

sDISS = λT⋅ekk2 + 2⋅μT⋅eij⋅eij

C.  ELASTIC, PERFECTLY-PLASTIC SOLID

The formulation investigated here is the one appearing in the text, Theory of Perfectly Plastic Solids, by William Prager and Philip Hodge, Jr. (John Wiley & Sons, Inc., 1951).  The von Mises stress, VM, is defined to be,

σVM = 32σij⋅σij − 13⋅σkk2 = 32⋅σij−13⋅σkk⋅δij⋅σij−13⋅σkk⋅δij

And all possible stress states must be such that,

σVM ≤ σYP

where YP is the yield point of the material in tension, a constant.  The strain is split into two parts. The elastic strain, eEij, is directly related to the stress state while the plastic strain  rate, ePij, is adjusted to be proportional to the reduced stress, σij − 13⋅σkk⋅δij.  The total strain rate is the sum of the elastic strain rate and the plastic strain rate, eEij + ePij.  The relationship between the stress and the elastic strain is,

σij = λ⋅eEkk − 3⋅λ + 2⋅G⋅α⋅T-TO⋅δij + 2⋅G⋅eEij

or after inversion,

eEij = 12⋅G⋅σij+−μ2⋅1+μ⋅G⋅σkk+α⋅T-TO⋅δij

where the material parameter nomenclature is generally the same nomenclature used for the thermoelastic material considered above.  The plastic strain changes over a loading increment when σVM = σYP during the increment.  This change is governed by,

ePij = Γ⋅σij − 13⋅σkk⋅δij	while σVM = σYP

ePij = 0			otherwise

where  must be adjusted so that σVM = σYP at the end of the increment.  Note that ePkk = 0 so that the plastic strains contribute nothing to the rate of volume change.  The rate of doing external work for the elastic strain is assumed to be recoverable while the rate of doing work for the plastic strain is assumed to be dissipated into a heat flow rate within the material element.  Define these as,

WE = −σij⋅eEij = −λ⋅eEkk − 3⋅λ + 2⋅G⋅α⋅T-TO⋅eEkk − 2⋅G⋅eEij⋅eEij

WP = −σij⋅ePij = −2⋅G⋅eEij⋅Γ⋅σij − 13⋅σkk⋅δij = −4⋅G2⋅Γ⋅eEij⋅eEij−13⋅eEkk2	 while σVM = σYP

WP = 0						 otherwise

Now assume that the internal energy, E, is a function of the elastic strain, eEij, and the temperature T.  For this material the First Law of Thermodynamics is written as,

q = E + WE

so that,

q = ∂ E∂eEij − λ⋅eEkk − 3⋅λ + 2⋅G⋅α⋅T-TO⋅δij − 2⋅G⋅eEij⋅eEij + ∂ E∂T⋅T

and,

s = 1T⋅∂ E∂eEij − λ⋅eEkk − 3⋅λ + 2⋅G⋅α⋅T-TO⋅δij − 2⋅G⋅eEij⋅eEij + 1T⋅∂ E∂T⋅T

In order for the entropy to be a property,

−1T2⋅∂ E∂eEij − λ⋅eEkk − 3⋅λ + 2⋅G⋅α⋅T-TO⋅δij − 2⋅G⋅eEij + 1T⋅∂2 E∂T ∂eEij + 3⋅λ + 2⋅G⋅α⋅δij 1T⋅∂2 E∂eEij ∂T

As usual, the order of differentiation of the second derivatives is assumed interchangeable so that,

∂ E∂eEij = λ⋅eEkk⋅δij + 2⋅G⋅eEij+3⋅λ+2⋅G⋅α⋅TO⋅δij

When this equation is integrated there results,

E = 12⋅λ⋅eEkk2 + G⋅eEij⋅eEij +3⋅λ+2⋅G⋅α⋅TO⋅Ekk+ KT

and,

q = 3⋅λ + 2⋅G⋅α⋅T⋅eEkk + d KTdT⋅T

s = 3⋅λ + 2⋅G⋅α⋅eEkk + 1T⋅∂ KT∂T⋅T

Now define a specific heat at constant volume, cV, using,

q|eEkk=0 = cVT

to obtain,

cV = d KTdT

where, obviously, cV is a function of temperature only.  The heat flow rate and entropy production rate may be written as,

q = 3⋅λ + 2⋅G⋅α⋅T⋅eEkk + cV⋅T

s = 3⋅λ + 2⋅G⋅α⋅eEkk + 1T⋅cV⋅T

Similar to the case for a fluid, the quantity q is the total heat flow rate in the material element.  The quantity WP is the rate of work for the plastic strain that is converted to a heat flow rate.  Let q be the externally supplied heat flow rate so that,

If σVM = σYP:

q = q − WP = 3⋅λ + 2⋅G⋅α⋅T⋅eEkk + cV⋅T + 4⋅G2⋅Γ⋅eEij⋅eEij − 13⋅eEkk2

and,

sTOT = 3⋅λ + 2⋅G⋅α⋅eEkk + cV⋅TT + 4⋅G2⋅ΓT⋅eEij⋅eEij − 13⋅eEkk2

sDISS = sTOT−s = 4⋅G2⋅ΓT⋅eEij⋅eEij − 13⋅eEkk2

otherwise:

q = 3⋅λ + 2⋅G⋅α⋅T⋅eEkk + cV⋅T

sTOT = 3⋅λ + 2⋅G⋅α⋅eEkk + 1T⋅cV⋅T

sDISS = sTOT−s = 0

D.  INCOMPRESSIBLE BINGHAM MATERIAL.

The most common formulation for this material neglects thermal expansion and elastic behavior of the material and this approximation is adopted here.  The specific heat, cV. is assumed to be constant.  This material has a yield point stress that must be exceeded before the material can deform.  When the yield stress is exceeded, the material flows similar to a fluid but with the flow rate proportional to the excess of the stress over the yield point stress.  Let,

σVM = 32⋅σij⋅σij − 12⋅σkk2 = 32⋅σij⋅σij − 13⋅σkk2 ≡ 3⋅τVM

where VM is the von Mises stress in tension and VM is the von Mises stress in shear.  The yield point stress in shear is the value of the von Mises stress in simple shear that causes yielding of the material.  For this material it is common to formulate the constitutive equation in terms of the constant value of YP.  The constitutive equation for the incompressible Bingham material is.

2⋅μ⋅eij = σVM − 3⋅τYPσVM⋅σij − 13⋅σkk⋅δij		when σVM ≥ 3⋅τYP

2⋅μ⋅eij = 0						otherwise

When this material undergoes deformation, the entire rate of work done by the stresses is converted to a heat flow rate.  Consequently, in the First Law of Thermodynamics for the material W = 0.  In addition, the internal energy is assumed to be a function of temperature only.  Under these conditions, the first law becomes,

q = ∂ E∂T⋅T

and the entropy production rate is,

s = ∂ E∂T⋅TT

Clearly, ∂ E∂T may be interpreted as the specific heat at constant volume, cV, and it is assumed to have a constant value so that,

E = cV⋅T−TO

q = cV⋅T

s = cV⋅TT

During deformation, the quantity -σij⋅eij is the heat flow rate internal to the material element and,

-σij⋅eij = σVM − 3⋅τYP2⋅μ⋅σVM⋅σij⋅σij − 13⋅σkk2 = σVM − 3⋅τYP⋅σVM3⋅μ , σVM ≥ 3⋅τYP

= 0 ,								         otherwise

so that the externally supplied heat flow rate, q, is,

q = cV⋅T + σVM − 3⋅τYP⋅σVM3⋅μ 	, σVM ≥ 3⋅τYP

q = cV⋅T 				, otherwise

and,

sTOT = cV⋅TT + σVM − 3⋅τYP⋅σVM3⋅μ⋅T 	, σVM ≥ 3⋅τYP

sTOT = cV⋅TT 					, otherwise

Owing to the assumption of incompressibility the mean stress, 13⋅σkk, is indeterminate from the deformation. A similar situation occurs in the case of any incompressible material.

The last two equations may be written more compactly using Macaulay brackets as,

sTOT = cV⋅TT + σVM − 3⋅τYP⋅σVM3⋅μ⋅T	and 	sDISS = σVM − 3⋅τYP⋅σVM3⋅μ⋅T

Where the added brackets are defined as,

x = x when x≥ 0 and x = 0 otherwise

E.  PENG-ROBINSON CUBIC EQUATION OF STATE

This equation is used frequently to represent the state of the material in vapor-liquid equilibrium calculations for the oil industry.  No viscous effects are included here.  For a specified state (vapor or liquid) the equation contains three constants, R, a and b.  It relates the pressure, p, to the specific volume, v, and absolute temperature, T, as follows,

p = R⋅Tv − b − av2 + 2⋅b⋅v − b2

A consistent set of units is,

p	lbfin2			R	in0R

T	oR			b	in3lbf

v	in3lbf			a	in4lbf

For this case, assume the internal energy is a function of the specific volume and the temperature, E = E(v, T).  With

W = rate of doing work = p⋅v

the First Law of Thermodynamics yields,

q = ∂ E∂v + p⋅v + ∂ E∂T⋅T

and then,

s =qT = 1T⋅∂ E∂v + p⋅v + ∂ E∂T⋅TT

In order for the entropy to be a state variable,

-1T2⋅∂ E∂v + p + 1T⋅∂2 E∂T ∂v + ∂ p∂T = 1T⋅∂2 E∂v ∂T

The second derivatives are independent of the order of differentiation so that,

∂ E∂v + p − T⋅∂ p∂T = 0

When p is eliminated from this equation using the equation of state, the result is,

∂ E∂v = av2 + 2⋅b⋅v − b2

and integration gives,

E = a8⋅b2⋅ln2⋅v + 2⋅b − 8⋅b22⋅v + 2⋅b + 8⋅b2 + LT = a2⋅2⋅b⋅lnv + 1-2⋅bv + 1+2⋅b+LT

so that

q = R⋅Tv − b⋅v + dLTdT⋅T

The multiplier of T is the specific heat at constant volume, cV, so the heat flow rate and entropy production rate become, for constant cV,

q = R⋅Tv − b⋅v + cV⋅T

s = qT = Rv − b⋅v + cV⋅TT

Since there is no energy dissipation for this material,

q = q = R⋅Tv − b⋅v + cV⋅T

and,

sTOT = s = Rv − b⋅v + cV⋅TT

Note that, when a = b = 0, the Peng-Robinson equation reduces to the ideal gas law.  Also note that van der Waals’ equation cannot be recovered from the Peng-Robinson equation as a special case.

F.  VOIGT MATERIAL (KELVIN-VOIGT MATERIAL)

The sketch below is a conceptual description of this material.  Although it is helpful to represent the physical characteristics of the material with this sort of sketch, D. C. Drucker (Second-order Effects in Elasticity. Plasticity and Fluid Dynamics, International Symposium, Haifa, Israel, April 23-27, 1962) has pointed out the limitations of material models based on such sketches.

The contributions to the stress, Eij, and Vij, are taken as the classical, linear formulations for thermoelastic and viscous materials.  The external work is associated with Eij only.  The work associated with Vij is dissipated as heat in the material element.   The total stress is the sum of the two contributions so,

σEij = λ⋅ekk − 3⋅α⋅T⋅δij + 2⋅G⋅eij − α⋅T⋅δij

σVij = λ⋅ekk⋅δij + 2⋅μ⋅eij

σij = σEij + σVij

The internal energy, E, is assumed to be a function of Eij and T only.  The work term is taken as −σEij⋅eij and then the First Law of Thermodynamics becomes.

q = ∂ E∂eij − σEij⋅eij + ∂ E∂T⋅T

and

s = qT = 1T⋅∂ E∂eij − σEij⋅eij + ∂ E∂T⋅TT

The condition that must be satisfied in order that the entropy, s, be a state variable is,

-1T2⋅∂ E∂eij − σEij + 1T⋅∂2 E∂T ∂eij − ∂ σEij∂T = 1T⋅∂2 E∂eij ∂T

The order of differentiation for the second derivatives may be interchanged so this condition becomes,

∂ E∂eij = σEij − T⋅∂ σEij ∂T

When the constitutive equation for the elastic part of the strain is substituted into this condition, the result is,

∂ E∂eij = λ⋅ekk⋅δij + 2⋅G⋅eij

and integration gives,

E = 12⋅λ⋅ekk2 + G⋅eij⋅eij + MT

with M(T) being an arbitrary function of temperature.  Recognizing that the specific heat at constant volume, cV, is related to M(T) through,

d MTdT = cV

yields,

q = 3⋅λ + 2⋅G⋅α⋅T⋅ekk + cV⋅T

s = 3⋅λ + 2⋅G⋅α⋅ekk + cV⋅TT

Since the internally generated heat flow rate is −σVij⋅eij, the external heat flow rate, q, is given by,

q = q + σVij⋅eij = q + λ⋅ekk2 + 2⋅μ⋅eij⋅eij = 3⋅λ + 2⋅G⋅α⋅T⋅ekk + cV⋅T + λ⋅ekk2 + 2⋅μ⋅eij⋅eij

and,

sTOT = 3⋅λ + 2⋅G⋅α⋅ekk + cV⋅TT + λT⋅ekk2 + 2⋅μT⋅eij⋅eij

and,

sDISS = sTOT−s = λT⋅ekk2 + 2⋅μT⋅eij⋅eij

G.  MAXWELL MATERIAL

The sketch below gives a conceptual, physical understanding of the Maxwell material.  The strain has separate elastic and viscous components, eEij and eVij, that are induced by the total stress, ij.

The analytical model developed here uses classical, linear definitions to relate ij, eEij, eVij and T as follows,

σij = λ⋅eEkk − 3⋅α⋅T⋅δij + 2⋅G⋅eEij − α⋅T⋅δij

σij = λ⋅eVkk⋅δij + 2⋅μ⋅eVij

and the total strain rate, eij, is defined as,

eij = eEij + eVij

The external rate of work is −σij⋅eEij while the internal rate of work that is converted to heat flow rate is −σij⋅eVij.

σij⋅eEij = λ⋅eEkk⋅eEmm+2⋅G⋅eEij⋅eEij−3⋅λ+2⋅G⋅eEkk

σij⋅eVij = λ⋅eVkk2+2⋅μ⋅eVij⋅eVij

The internal energy, E, is assumed to be a function of eEij and T only.  The First Law of Thermodynamics for this formulation is,

q = ∂ E∂eEij − σij⋅eEij + ∂ E∂T⋅T

and

s = qT = 1T⋅∂ E∂eEij − σij⋅eEij + ∂ E∂T⋅TT

The condition that entropy be a state variable is,

−1T2⋅∂ E∂eEij − σij + 1T⋅∂2 E∂T ∂eEij − ∂ σij∂T = 1T⋅∂2 E∂eEij ∂T

The order of differentiation may be interchanged so this equation becomes,

∂ E∂eEij = σij − T⋅∂ σij∂T

Substitution of the constitutive equation for the elastic part of the strain into this equation gives,

∂ E∂eEij = λ⋅eEkk⋅δij + 2⋅G⋅eEij

and integration leads to,

E = 12⋅λ⋅eEkk2 + G⋅eEij⋅eEij + NT

The function of integration, N(T), is related to the specific heat at constant volume, cV, through,

cV = d NTdT

so that,

q = 3⋅λ + 2⋅G⋅α⋅T⋅eEkk + cV⋅T

s = 3⋅λ + 2⋅G⋅α⋅eEkk + cV⋅TT

The external heat flow rate, q, is the difference between the total heat flow rate, q, and the internal heat flow rate, −σij⋅eVij, so that,

q = q + σij⋅eVij = q + λ⋅eVkk2 + 2⋅μ⋅eVij⋅eVij = 3⋅λ + 2⋅G⋅α⋅T⋅eEkk + cV⋅T + λ⋅eVkk2 + 2⋅μ⋅eVij⋅eVij

and,

sTOT = 3⋅λ + 2⋅G⋅α⋅eEkk + cV⋅TT + λT⋅eVkk2 + 2⋅μT⋅eVij⋅eVij

where,

eEkk = σkk3⋅λ+2⋅G+3⋅α⋅T

eVkk2 = σkk23⋅λ+2⋅μ2

eVij⋅eVij = 3⋅λ⋅σkk2⋅μ⋅3⋅λ+2⋅μ2−λ⋅σkk22⋅μ2⋅3⋅λ+2⋅μ+σij⋅σij4⋅μ2 = σij⋅σij4⋅μ2−λ⋅3⋅λ+4⋅μ⋅σkk24⋅μ2⋅3⋅λ+2⋅μ2

λ⋅eVkk2+2⋅μ⋅eVij⋅eVij = σij⋅σij2⋅μ−3⋅λ2⋅σkk24⋅μ⋅3⋅λ+2⋅μ2

sTOT = 3⋅λ + 2⋅G⋅α⋅eEkk + cV⋅TT +σij⋅σij2⋅μ⋅T−3⋅λ2⋅σkk24⋅μ⋅3⋅λ+2⋅μ2⋅T

and,

sDISS = sTOT−s = σij⋅σij2⋅μ⋅T−3⋅λ2⋅σkk24⋅μ⋅3⋅λ+2⋅μ2⋅T

III.  IRREVERSIBLE THERMODYNAMICS RESULTS FOR SOME COMMON ENGINEERING MATERIAL MODELS UNDERGOING CHANGES IN THERMODYNAMIC EQUILIBRIUM

INTRODUCTION

The definition of a reversible thermodynamic process for a constant, unit mass system is that the rate of change of the system entropy, s, during the process is given by,

s = sREV ≡ QREVT ≤ QT

where a superposed dot implies rate of change,

T	= absolute temperature

s	= actual rate of change of entropy of system

sREV	= corresponding rate of change of entropy during a reversible process

Q	= actual rate of heat flow into system

QREV	= corresponding rate of heat flow into system undergoing a reversible process

s, sREV, Q and QREV are all expressed as per unit volume quantities.

An expression determining sREV for a homogenous material with defined properties may be found as described above using the First Law of Thermodynamics for a reversible system as,

sREV = 1T⋅E+1T⋅WREV

where,

E 	= rate of internal energy per unit volume increase of the material per unit mass.

The internal energy, E, is a state variable.

WREV	= rate of doing work per unit volume by system (with constitutive equation

satisfied).  Instantaneous constitutive equation satisfaction implies instantaneous

equilibrium states.  The constitutive equation (equation of state) defines the

possible equilibrium states for the material.

The internal energy per unit volume of a homogeneous material is part of the definition of the material.  It may be specified, for example, as being a function of strain, eij, and temperature, T.  The specification of the variables defining E are based on the physical understanding of the material being modeled.

The expression for WREV may be determined using the constitutive equation for the material.  Since the constitutive equation defines only equilibrium states it satisfies the required condition onWREV.

When the formulations for E and WREV are substituted into the above equation for the First Law of Thermodynamics for a reversible system, an equation for sREV is found.  The validity of this equation may be evaluated using a fundamental postulate of thermodynamics.  The postulate is that sREV is a property of the material (not path dependent).  For example, when the expressions for E and WREV are,

E = ∂ E∂eij⋅eij+∂ E∂T⋅T

WREV = −σij⋅eij

where σij is a stress component then,

sREV = 1T⋅∂ E∂eij−σij⋅eij+1T⋅∂ E∂T⋅T

If sREV is a state property, its differential must be an exact differential and expressible as,

sREV = ∂ sREV∂eij⋅eij+∂ sREV∂T⋅T

Comparison of the last two equations shows that,

∂∂T1T⋅∂ E∂eij−σij = ∂∂eij1T⋅∂ E∂T

The last equation is a partial differential equation for E(ij, T).  Since the second derivative is independent of the order of differentiation the equation reduces to,

∂ E∂eij = σij+∂ E∂T

When the constitutive equation is substituted into the last equation, ∂ E∂eij is found explicitly and E can be determined by integration of this equation.  Clearly, the procedure just described requires that E, WREV and the constitutive equations be compatible so that E may be determined as a property of the material.

One extension to the formulation above may be found in the theory of Irreversible Thermodynamics.  When this theory is limited to processes that are approximated as being instantaneously in equilibrium (i.e. satisfy the constitutive equations at every instant), the results presented below are obtained using the concept of a dissipative term in the First Law of Thermodynamics.  The equations used here for this irreversible process can be derived by splitting the heat flow rate into two parts.  The first is QREV where it is assumed that the state variable, E, has been determined and sREV is determined as described above and,

QREV = T⋅sREV

The second part of the heat flow, QDISS, is defined in terms of the actual rate of change of entropy, s as,

QDISS = T⋅s−sREV ≡ T⋅sDISS

Consequently, the actual heat flow rate into the system, Q, is,

Q = QREV+QDISS = T⋅s

The results reported in the preceding section included the procedures given in this section without introducing the formalities of Irreversible Thermodynamics.  The tabulation below summarizes the results of the preceding section.  For each of the seven material models studied the following tabulation gives,

- the constitutive equation

- the equation for the internal energy. E

- the reversible rate of change of entropy, sREV

- the total rate of change of entropy, sTOT

- the dissipative rate of change of entropy, sDISS

The slight changes in the nomenclature below are obvious.  Two of the seven materials in the following tabulation have sDISS = 0 (linear thermoelasticity and Peng-Robinson).  In Irreversible Thermodynamic theory the expressions for sDISS are generalized using Onsager’s relations, to be introduced later, that include non-equilibrium states.  When the constitutive equations are satisfied at every instant, sDISS determines the coefficients for the Onsager relations.

A.  LINEAR THERMOELASTICITY

σij = λ⋅ekk − 3⋅α⋅T⋅δij + 2⋅G⋅eij − α⋅T⋅δij

E = 12⋅λ⋅ekk2+G⋅eij⋅eij+cV⋅T−TO

sREV = 3⋅λ+2⋅G⋅α⋅ekk+cV⋅TT

sTOT = 3⋅λ+2⋅G⋅α⋅ekk+cV⋅TT

sDISS = 0

B.  LINEAR, VISCOUS, COMPRESSIBLE NEWTONIAN FLUID

σij = λ⋅ekk⋅δij + 2⋅μ⋅eij + C⋅ekk − 3⋅α⋅T⋅δij

E = 12⋅C⋅ekk2+cV⋅T−TO

sREV = 3⋅α⋅C⋅ekk+cV⋅TT

sTOT = 3⋅α⋅C⋅ekk+cV⋅TT+λT⋅ekk2+2⋅μT⋅eij⋅eij

sDISS = λT⋅ekk2+2⋅μT⋅eij⋅eij

C.  ELASTIC, PERFECTLY-PLASTIC SOLID

σVM = 32⋅σij⋅σij − 12⋅σkk2 = 32⋅σij−13⋅σkk⋅δij⋅σij−13⋅σkk⋅δij	( adjusted to ensure this condition)

eij = eEij+Γ⋅σij−13⋅σkk⋅δij

σij = λ⋅eEkk − 3⋅λ + 2⋅G⋅α⋅T-TO⋅δij + 2⋅G⋅eEij

or

eEij = σij2⋅G+−λ3⋅λ+2⋅G⋅σkk2⋅G+α⋅T-TO⋅δij

E = 12⋅λ⋅eEkk2+G⋅eEij⋅eEij+3⋅λ+2⋅G⋅α⋅TO⋅eEkk+cV⋅T−TO

sREV = 3⋅λ+2⋅G⋅α⋅eEkk+cV⋅TT

sTOT = 3⋅λ+2⋅G⋅α⋅eEkk+cV⋅TT+4⋅G2⋅ΓT⋅eEij⋅eEij−13⋅eEkk2

sDISS = 4⋅G2⋅ΓT⋅eEij⋅eEij−13⋅eEkk2 = ΓT⋅σij⋅σij−13⋅σkk2+16⋅G23⋅λ+2⋅G⋅σkk⋅α⋅T =ΓT⋅23⋅σVM2+16⋅G23⋅λ+2⋅G⋅σkk⋅α⋅T

D.  INCOMPRESSIBLE BINGHAM MATERIAL

σVM = 32⋅σij⋅σij − 12⋅σkk2 = 32⋅σij⋅σij − 13⋅σkk2 ≡ 3⋅τVM

2⋅μ⋅eij = σVM − 3⋅τYPσVM⋅σij − 13⋅σkk⋅δij		when σVM ≥ 3⋅τYP

2⋅μ⋅eij = 0						otherwise

E = cV⋅T−TO

sREV = cV⋅TT

sTOT = cV⋅TT+σVM−3⋅τYP⋅σVM3⋅μ⋅T		σVM ≥ 3⋅τYP

sTOT = cV⋅TT						otherwise

sDISS = σVM−3⋅τYP⋅σVM3⋅μ⋅T				σVM ≥ 3⋅τYP

sDISS = 0						otherwise

E.  PENG-ROBINSON CUBIC EQUATION OF STATE

p = R⋅Tv − b − av2 + 2⋅b⋅v − b2

E = a2⋅2⋅b⋅lnv+1−2⋅bv+1+2⋅b

sREV = Rv−b⋅v+cV⋅TT

sTOT = Rv−b⋅v+cV⋅TT

sDISS = 0

F.  VOIGT MATERIAL (KELVIN-VOIGT MATERIAL)

σEij = λ⋅ekk − 3⋅α⋅T⋅δij + 2⋅G⋅eij − α⋅T⋅δij

σVij = λ⋅ekk⋅δij + 2⋅μ⋅eij

σij = σEij + σVij

E = 12⋅λ⋅ekk2+G⋅eij⋅eij+cV⋅T−TO

sREV = 3⋅λ+2⋅G⋅α⋅ekk+cV⋅TT

sTOT = 3⋅λ+2⋅G⋅α⋅ekk+cV⋅TT+λT⋅ekk2+2⋅μT⋅eij⋅eij

sDISS = λT⋅ekk2+2⋅μT⋅eij⋅eij

G.  MAXWELL MATERIAL

σij = λ⋅eEkk − 3⋅α⋅T⋅δij + 2⋅G⋅eEij − α⋅T⋅δij

σij = λ⋅eVkk⋅δij + 2⋅μ⋅eVij	   or	eVij = 12⋅μ⋅σij−λ2⋅μ⋅3⋅λ+2⋅μ⋅σkk⋅δij

and the total strain rate, eij, is defined as,

eij = eEij + eVij

E = 12⋅λ⋅eEkk2+G⋅eEij⋅eEij+cV⋅T−TO

sREV = 3⋅λ+2⋅μ⋅α⋅eEkk+cV⋅TT

sTOT = 3⋅λ+2⋅μ⋅α⋅eEkk+cV⋅TT+λT⋅eVkk2+2⋅μT⋅eVij⋅eVij = 3⋅λ + 2⋅G⋅α⋅eEkk + cV⋅TT +σij⋅σij2⋅μ⋅T−3⋅λ2⋅σkk24⋅μ⋅3⋅λ+2⋅μ2⋅T

sDISS = λT⋅eVkk2+2⋅μT⋅eVij⋅eVij= σij⋅σij2⋅μ⋅T−3⋅λ2⋅σkk24⋅μ⋅3⋅λ+2⋅μ2⋅T

IV.  NON-EQUILIBRIUM THERMODYNAMICS

The subject of Non-Equilibrium Thermodynamics considers thermodynamic systems that are not at all instants in equilibrium (don’t satisfy the constitutive equations).  The preceding sections have dealt with dissipation resulting from viscous flow and plastic flow.  In all of the above cases the entropy dissipation can be expressed in terms of state variables or their time derivatives (σij,σij or eij).  In this section the conceivably more complicated case of predicting behavior when the instantaneous state is not in equilibrium is considered.

The publication most frequently cited in this field is the book Non-Equilibrium Thermodynamics by S. R. de Groot and P. Mazur (Dover Publications, 1984).  This book presents the classical approach by using the difference between the total entropy rate and the reversible entropy rate as the measure of the non-equilibrium state.  In this book the measure is designated by  called”entropy production” and, according to the Second Law of Thermodynamics, must be  0.  For cases considered by de Groot and Mazur the entropy production is restricted to the form,

σ = i=1i=mJi⋅Xi

where Ji is a flux, Xi is a corresponding thermodynamic force and i is summed over all the m non-equilibrium influences.  The fluxes are assumed to be expressible in the phenomenological equations as,

Ji = i=1i=mLij⋅Xj

and the quantities Lij are called the phenomenological coefficients.  Eliminating Ji in the two preceding equations gives.

σ = i=1i=mi=1i=mLij⋅Xi⋅Xj

de Groot and Mazur give numerous examples and show that in many cases, but not all cases, the Onsager Reciprocal Relations are satisfied.  The Onsager Reciprocal Relations are that Lij is a symmetric matrix, that is,

Lij = Lji

So that the phenomenological coefficients are symmetric

The single case studied below has the constitutive equations completely specified.  This case is in this category of materials with memory. The behavior of these materials depends on the past loading history.  When the loading is removed at a specified time the material may continue to deform after that time.  The paper describing the constitutive equation and giving some comparisons with experiments can be described as an incompressible, gelling, Bingham material.  The constitutive equations are, using Macaulay brackets,

2⋅μ⋅dij = J2−τCRITJ2⋅σij−13⋅σkk⋅δij

where,

x	= x if x > 0; = 0 otherwise

	= a viscosity type constant, > 0

dij	= component of deformation rate, in terms of velocity components vi,

= 12⋅vi,j+vj,i

σij	= component of the stress tensor

J22	= second invariant of the reduced stress tensor

= 12⋅σij−13⋅σkk⋅δij⋅σij−13⋅σkk⋅δij

τCRIT = yield point in shear at time t, time, dependant yield point in shear =τ1−ξ = −∞ξ = tD2⋅e−α⋅t−ξ⋅d ξβ+ξ = −∞ξ = tD2⋅e−α⋅t−ξ⋅d ξ⋅τ1−τ0

t	= current time

	= dummy variable for time

	= time constant , > 0

	= a constant in the equation for CRIT,  0

D22	= second invariant of deformation rate tensor

= 12⋅dij⋅dij

1	= fully gelled yield point in shear,  0

0	= minimum achievable yield point in shear,  0

The rate of doing external work by the stresses, W, is,

W = σij⋅dij = J2−τCRIT2⋅μ⋅J2⋅σij⋅σij−13⋅σkk2 = J2−τCRIT2⋅μ⋅J2⋅J2 =J2−τCRIT2⋅μ⋅J2

The specific heat, cV, is assumed to be constant and the internal energy, E, is assumed to be a function of T only so the reversible rate of heating, qREV, is,

qREV = d EdT⋅T = cV⋅T

and,

sREV = cV⋅TT

Then,

qTOT = cV⋅T+J2−τCRIT2⋅μ⋅J2

and,

sTOT = cV⋅TT+J2−τCRIT2⋅μ⋅T⋅J2

so that,

sDISS = sTOT −sREV= J2−τCRIT2⋅μ⋅T⋅J2

Comparing this result given above for the non-equilibrium formulation, realizing that σ = sDISS and that m = 1 gives,

σ = L11⋅X12 = J2−τCRIT2⋅μ⋅T⋅J2

so that acceptable choices for L11 and X1 are,

X1 = J2μ

L11 = 12⋅T⋅1 − τCRITJ2

Similar to the earlier cases for different materials, sDISS is non-vanishing when there are viscous influences in the material behavior.  In the other cases an equilibrium state (i. e.-

sDISS = 0 ) can be found by setting the deformation rate to zero.  On the other hand, the value of CRIT is dependent on the past history of the deformation rate so an equilibrium state cannot generally be established instantaneously.

For this gelling material it is clear that sDISS will not vanish when there has been a non-vanishing deformation rate.  When a constant, non-vanishing deformation rate is imposed for a long time, sDISS for the material will approach a constant value denoted here as the steady state value.  To illustrate how a steady state condition may be determined, consider this material in a viscometer that imposes a constant shear deformation rate.  Furthermore, idealize this deformation rate as a single non-trivial component, dxy, imposed sinceξ = −∞.  The value of CRIT can be found from D2 being constant (= D0) and D0 = +dxy to be,

τCRIT = τ1−ξ = −∞tD0⋅e−α⋅t−ξ⋅d ξβ+ξ = −∞tD0⋅e−α⋅t−ξ⋅d ξ⋅τ1−τ0 = τ1⋅α⋅βα⋅β+D0+τ0⋅D0α⋅β+D0 = τ1⋅α⋅βα⋅β+dxy+τ0⋅dxyα⋅β+dxy

For this deformation rate history the constitutive equations give,

σxx=σyy=σzz	and	xy

as the only non-trivial stress components.  Other than being equal to one another, the normal stresses are indeterminate from the constitutive equations because the material is incompressible.  For this steady state the shear stress, xy, and all components of the deformation rate are time independent.  The x-y constitutive equation becomes,

σxy = τCRIT+2⋅μ⋅dxy = τ1⋅α⋅βα⋅β+dxy+τ0⋅dxyα⋅β+dxy+2⋅μ⋅dxy

or,

σxyτ1 = 11+dxyα⋅β+τ0τ1⋅dxyα⋅β1+dxyα⋅β+2⋅μ⋅α⋅βτ1⋅dxyα⋅β ,	1 ≥ τ0τ1 ≥ 0

The two figures below are based on the last equation.  The first figure shows the influence of viscosity when 0 = 0 and the second shows the influence of τ0τ1 when μ⋅α⋅βτ1 = 0.25.

A second example illustrating the determination of the variation of sDISS with time is presented at this point.  For this example, the only non-vanishing component of the deformation rate is dxy > 0.  The time history for dij is defined in the sketch below.

The integral determining CRIT for t > t* is,

ξ = −∞ξ = tD2⋅e−α⋅t−ξ⋅d ξ = ξ = −∞tDA⋅e−α⋅t−ξ⋅d ξ+ξ = tξ = tDBe−α⋅t−ξd ξ = 1α⋅DB−DB−DAe−α⋅t−t

so that for t > t* ,

τCRIT = τ1+DB−DB−DA⋅e−α⋅t−tα⋅β+DB−DB−DAe−α⋅t−tτ1−τ0

and,

σxy = τCRIT+2⋅μ⋅DB

The last equation, in dimensionless form after eliminating τCRIT, becomes,

σxyτ1 = 1−ΔDDB⋅e−α⋅t−tα⋅βDB+1−ΔDDBe−α⋅t−t1−τ0τ1 +1+2⋅μ⋅DBτ1 ,		(t – t*) > 0

The above results may be used to evaluate the rate of dissipative entropy, sDISS, when t > t* as,

sDISS = J2−τCRIT2⋅μ⋅T⋅J2 = σxy−τCRIT2⋅μ⋅T⋅σxy = DB⋅σxyT

The figure below gives time histories of σxy−2⋅μ⋅DBτ1 for different values of ΔDDB when α⋅βDB = 0.5 and τ0τ1 = 0.

V.  OBSERVATIONS CONCERNING NON-EQUILIBRIUM THERMODYNAMICS

The customary presentation and treatment of Non-Equilibrium Thermodynamics is exemplified in de Groot and Mazur’s treatise, cited earlier.  Examples of many phenomena are presented including thermal conduction, chemical reactions and magnetic fields.  A change of state is usually accompanied by a change of entropy.  The excess of this change over the corresponding reversible change is expressed as the sum of products of “thermodynamic forces” and “thermodynamic displacements”.  A linear relationship between these forces and displacements is postulated in every case.  Many phenomena, but not all, are shown to satisfy the Onsager Reciprocal Relations.

In continuum mechanics the typical investigation proceeds differently from the scheme described in de Groot and Mazur’s treatise.  The common, practical, continuum mechanics investigation begins with a specified, defining constitutive equation and a compatible internal energy.  The internal energy is compatible when it and the constitutive equation can be used with the First Law of Thermodynamics to derive an expression for the entropy that is a path independent variable.  The preceding section presents a case of a gelling material.  The gelling strength, τCRIT, depends on the past history of an invariant of the deformation rate.  The only time an equilibrium state (that is, sDISS = 0) is reached, in a practical sense, is when there has been no shearing for a long time. The presence of a practical, steady state behavior is predicted for the gelling material when a constant, non-vanishing deformation rate is maintained for a long time.  Two illustrative examples are given above to demonstrate that the special tools of non-equilibrium thermodynamics are not required for many continuum mechanics study.

THIS IS FILE: IrrevThermo.doc

Available from website: http://www.drpaulpaslay.com/home

W. H. Macaulay, “Note on the Deflection of Beams”, The Messenger of Mathematics, v. 48, p. 129, 1919

* A. Slibar and P. R. Paslay, "On  the  Analytical  Description  of  the  Flow  of  Thixotropic Materials", Second-order Effects in Elasticity, Plasticity and Fluid Dynamics,  International Symposium,  Haifa,  Israel,  April 23-27, (1962) pp. 314-330.

See also H. C. H. Darley and George R. Gray, Composition and Properties of Drilling and Completion Fluids, Fifth Edition, Gulf Publishing Company, 1988, pp. 203,204.